Tender Descriptive:

- PONZI ALU FRAME -

ALU FRAME HOSPITAL SWING DOOR

SWING DOOR PONZI ALU FRAME TYPE

Made in a single / two swing leaf / s. Built with extruded profiles in ENAW 6060 aluminum alloy according to

UNI 9006/1 rules and accessories belonging to the ALU PONZI system. The profiles will be anodised, silver color

ARS1, class 15 micron according to UNI4522 regulation.

The door is complete with:

• Filling on three sides, with complementary extruded profiles that can be coupled together, suitable for wrapping the entire shoulder of the wall for a thickness from 100 to 150 mm (for higher wall thicknesses it will be compensated separately with extra charge).

• Door leaf, surrounded on all four sides by an aluminum frame with rounded edges of 45/50 mm; panel with internal core in high-density self-extinguishing Class 1 non-toxic polystyrene, double coating in HPL plastic thickness 0.9 mm, supported by a 4 mm MDF slab.

• Accessories: aluminum system hinges, Yale type lock, aluminum handle pair and round aluminum nozzle.

• Double door gasket in EPDM elastomer.

N...... dimensions from mm……… x mm. H.

Srl

Seat:	48031 BAGNARA (RA)

VIA Gramsci, 26/A Tel. +39 0545 76009

Fax +39 0545 76827

P. IVA 02144680390

20123 MILANO

Viale G. D’Annunzio, 25

Tel. +39 02  8394231

Fax +39 02 89422342

00138 ROMA

Via Salaria, 1378

Tel. +39 06 88566005

Fax +39 0688560406

65015 MONTESILVANO (PE)

Via A. Moro, 6

Tel. +39 085 4483020

Fax. +39 085 4455895

www.ponzi-in.it 	info@ponzi-in.it